## Slide 1: What is a Mineral

## Slide 2: What is a Mineral
A naturally occurring chemical compound characterized by a definite crystalline structure

## Slide 3: A Mineral Species
Species: Corundum
Ideal Chemical Formula: Al2O3

## Slide 4: What would “idea” end-member corundum look like?

## Slide 5: What would “idea” end-member corundum look like?
How would you find out?

## Slide 6: Synthetic Pure Al2O3 is colorless
Daiichi-Dentsu Company Creator Optics

## Slide 7: Montana Corundum

## Slide 8: Properties?
Corundum crystal from India

## Slide 9: Properties?

## Slide 10: Color
Color leads us to three concepts:
Solid Solution
(Al1.97M3+0.03)Σ=2.00O3

## Slide 11: Color
Color leads us to three concepts:
Solid Solution
What Elements Are Present?
What factors to consider?
Notes: Charge, Ionic Radius

## Slide 12: Synthetic Al2O3 with Cr3+

## Slide 13: Synthetic Al2O3 with Cr3+

## Slide 14: Color
Color leads us to three concepts:
Solid Solution
(Al1.97M3+0.03)Σ=2.00O3
Al2O3 ↔ Cr2O3
corundum ↔ eskolaite

## Slide 15: Color
Color leads us to three concepts:
Solid Solution
Variety

## Slide 16: Color
Color leads us to three concepts:
Solid Solution
Variety: Red from Cr3+ = ruby

## Slide 17: Rubies
Photo Credits: Pala International

## Slide 18: Synthetic Ruby Boule
Growth Temp = 2053°C

## Slide 19: Ti3+ in corundum

## Slide 20: Fe3+ in corundum

## Slide 21: Cobalt in corundum

## Slide 22: Other Elements ?

## Slide 23: Other Elements

## Slide 24: Other Elements

## Slide 25: Other Elements

## Slide 26: Color
Color leads us to three concepts:
Solid Solution
Variety
Coupled Substitution: 2 Al3+ = M2+ + M4+

## Slide 27: Color
Color leads us to three concepts:
Solid Solution
Variety
Coupled Substitution: 2 Al3+ = Fe2+ + Ti4+

## Slide 28: Color
Color leads us to three concepts:
Solid Solution
Variety
Coupled Substitution: 2 Al3+ = Fe2+ + Ti4+
Known as sapphire

## Slide 29: Sapphire from Laos

## Slide 30: Sapphire Gems
Photo courtesy of Tairus.

## Slide 31: Sapphire from Tanzania

## Slide 32: Sapphire from Laos

## Slide 33: Other Elements

## Slide 34: Density
Density = ~4.0
nd = 1.76

## Slide 35: Hexagonal Close Packing

## Slide 36: Hexagonal Close Packing

## Slide 39: Isostructural

## Slide 40: Hematite
Fe2O3 isostructural with corundum

## Slide 41: Hematite
Fe2O3 isostructural with corundum
Brumado, Bahia, Brazil

## Slide 42: Hematite
Fe2O3 isostructural with corundum
An important
ore of iron
Carajas, Brazil

## Slide 43: Hematite Color

## Slide 44: Hematite Crystals
Notes: Cumberland England

## Slide 45: Massive Hematite
Cumberland, England
Notes: Cumberland England

## Slide 46: Hematite
Cumberland, England
Notes: Cumberland England

## Slide 47: Hematite
Michigan
Notes: Michigan

## Slide 48: The Hematite Optical Spectrum

## Slide 49: Particle Size

## Slide 50: Commercial Pigments

## Slide 51: Paint Strips
0.15 μm
2.5 μm

## Slide 52: Streak Test

## Slide 53: Important Pigment in Soil
NE coast of Brazil

## Slide 54: Hematite in Rock
Near Moab, Utah

## Slide 55: Ilmenite
FeTiO3
HCP
An important ore of titanium
Commonly found in both igneous and metamorphic rocks.
Concentrates in heavy mineral sands in rivers and beaches.
First found in the Ilmensky Mountains

## Slide 56
Ilmenite
Question:
Do Fe and Ti form
separate layers or
do they scramble?

## Slide 57: Ilmenite

## Slide 58: Exsolution

## Slide 59
Ilmenite in basalt is often a solid solution
e.g. Il80Hem20 = 0.8(Fe2+Ti4+O3) + 0.2(Fe3+Fe3+O3)

## Slide 60
Ilmenite in basalt is often a solid solution
e.g. Il80Hem20 = 0.8(Fe2+Ti4+O3) + 0.2(Fe3+Fe3+O3)
Envision a reaction: Fe2+Ti4+O3
Fe3+Fe3+O3
Fe2+Fe3+2O4 + TiO2
magnetite

## Slide 62
Or, the hematite could exsolve
Il80Hem20 = 0.8(Fe2+Ti4+O3) + 0.2(Fe3+Fe3+O3)
Fe2+Ti4+O3 + Fe3+2O3

## Slide 64: Rutile in Corundum
John Koivula in lotusgemology.com
TiO2 in Al2O3
Star sapphire
Photo Credit: Wikipedia Commons