# revision 9:45 am,  17-Sep-03

# OH in naturally occurring corundum

A. Beran1 and George R. Rossman

Division of Geological and Planetary Sciences,

California Institute of Technology, Pasadena, USA 91125-2500

1 Permanent address: Institut für Mineralogie und Kristallographie, Universität Wien-Geozentrum, Austria

Summary

OH bands arising from intrinsic hydrous defects have been observed in the infrared spectra of a number of corundum crystals from worldwide localities.  The OH defects are most prominent in blue sapphire crystals suggesting an association of OH with oxidation/reduction reactions involving iron. The absolute concentrations are generally 0.5 ppm or lower; the linear OH absorption coefficient for the most intense band centered at 3310 cm-1 never exceeds 0.005 cm-1. In addition to the intrinsic OH defects, a number of previously identified hydrous inclusions often contribute to absorptions in the OH stretching vibrational region of corundum.

Introduction

While it is now established that trace amounts of OH commonly occur in nominally anhydrous silicate minerals, there have been comparatively few studies of OH in the common oxide minerals.  Significant amounts of OH can occur in rutile (Hammer and Beran, 1991; Vlassopoulos et al., 1993; Maldener et al., 2001) and isolated instances of small amounts of OH have been reported in anatase, brookite, cassiterite (Beran and Zemann, 1971; Maldener et al., 2001), and manganese oxides (Potter and Rossman, 1979). Recognizing that there have been several reports of OH in synthetic corundum and occasional reports of OH in natural corundum, we undertook a study of naturally occurring corundum representing different varieties and geographic localities to ascertain if OH is a common component of this mineral and to determine the actual amount.

Colored varieties of corundum give us two of our most important gemstones: red rubies and a variety of sapphires in different colors and hues. Large synthetic single-crystals are grown for a variety of technological applications because of its superior hardness and optical transmission, among other reasons. Consequently, a variety of studies addressed the infrared transmission of corundum.

In synthetic corundum, OH groups are recognized both as a component of included phases and as a trace component of corundum itself.  Belt (1967) described broad absorption bands combined with several narrow bands in the OH region (3100 - 3600 cm-1) of the infrared spectrum of hydrothermally grown ruby and attributed two sharp bands at 3230 and 3180 cm-1 to the presence of monohydrate phases (boehmite, diaspore). Eigenmann et al. (1972) described OH bands in Verneuil sapphires at 3310, 3230, 3180 and 3025 cm-1 and Volynets et al. (1972) observed OH absorptions in the spectra of Verneuil-grown corundums with sharp bands at 3420, 3310, 3275, 3225 and 3160 cm-1. Polarized measurements of the sharp bands, now attributed to OH groups incorporated in the corundum structure, indicated that the OH groups causing them are aligned perpendicular to the c-axis.

A polarized IR-spectroscopic study of a suite of 22 Verneuil-grown corundums (Beran, 1991) found that variously colored corundums show a distinct variability in the region of the OH fundamental vibration.  Narrow, strongly polarized OH bands are centered at 3310, 3230 and 3185 cm-1 and are correlated to cation vacancies. Regarding this band as a triplet, two types of spectra are discernible; the type I spectrum is defined by a strong absorption band at 3230 cm-1 whereas the band at 3310 cm-1 is most prominent in type II spectrum.  Additional weak bands at 3290 cm-1 occur in (V, Cr, Fe, Ti)-doped "alexandrite" sapphires, weak bands at 3280 and 3160 cm-1 were observed in colorless and light rose corundum. Moon and Phillips (1991) described strong OH bands centered at 3309, 3232 and 3187 cm-1, and additional weak bands at 3367 and 3295 cm-1. The OH defects appear to be correlated to vacant Al sites and to the presence of tetravalent Ti (Moon and Phillips, 1994). Two distinct types of OH absorption bands were reported for hydrothermally treated synthetic sapphires by Kronenberg et al. (2000). The first type of bands is characterized by narrow bandwidths and strong polarizations with maximum absorbance measured perpendicular to the c-axis. Bands were observed at 3308, 3293, 3278, 3231, 3208, 3183, and 3163 cm-1. The second type of OH absorption consists of a broad isotropic band centered at 3400 cm-1, resembling closely the OH bands of hydrothermally grown quartz (Kronenberg, 1994).

There are also suggestions that OH may occur in natural corundum. Beran (1991) observed extremely weak OH absorptions at 3310, 3230 and 3185 cm-1 in the spectra of a ruby from Sri Lanka and a blue sapphire from Montana. Because the samples used in this study were faceted gemstones, is was not ascertained if these were corundums in their natural state or if they had been subjected to high-temperature heat treatment, a common practice in the manufacture of the corundum gemstones that can introduce OH at the same wavenumbers, particularly in treated sapphires (Emmett et al. 2003). Such concerns are justified in view of the observations of Smith (1995) and Peretti et al. (1995) of comparable sharp OH bands in heat treated ruby, but not in untreated natural samples. Further confirmation of OH in natural corundum is presented by Smith et al. (1995) who stated that OH bands are observed in the IR spectra of blue sapphires from basaltic sources in southern Vietnam, and Emmett et al. (2003) who report OH bands at 3367, 3310, 3233, and 3185 cm-1 in a pink sapphire from Vietnam. The present study represents an extension of the initial examination of natural corundums with better controlled histories.

Sample Description and Experimental

A collection of 150 corundum crystals, summarized in Table 1, was obtained from private collectors and museum collections with the objective of obtaining untreated crystals.  Many of these represented old collections believed to have been collected before the practice of heat treating corundum became common place. To clarify the question of the presence of OH in naturally occurring corundum, samples from a variety of different localities were studied.  Because of the earlier indications that OH may occur in Montana sapphires (Beran, 1991), we included a large number of sapphires from various Montana mines.

The samples were carefully cleaned but most were not ground and polished. Practically all crystals show rounded faces and most of them were elongated parallel to the c-axis. Thicknesses were generally in the range from 0.25 to 0.65 cm. The crystals were examined through different areas which varied from 100 to 600 µm in diameter. We examined samples ranging from gem quality to turbid or altered. Attempts were made to use an orientation that contained the c-axis, but this was not accomplished with all samples. Table 1 represents the linear absorption coefficient, ( (in cm-1), defined by ( = A/t where A is the linear absorbance (log[I0/I]) of the most intense and significant OH absorption band at 3310 cm-1 and t the thickness of the crystal measured in cm. The table presents the intensities of unpolarized spectra.

Unpolarized infrared spectra were recorded from 4000 to 2400 cm-1 on a Nicolet 60SX FTIR spectrometer operating at 2 cm-1 resolution. A ceramic light source, and a LN2 cooled MCT detector were used. Background and sample spectra were respectively obtained from 128 scans in air and through the sample crystal. For polarized measurements, a LiIO3 crystal polarizer was used with a Nicolet Magna 860 FTIR spectrometer with other details the same as for the unpolarized measurements.

Results and Discussion

The presence of significant absorption at 3310 cm-1 in the spectra of approximately one fifth of all studied samples proves that OH occurs in naturally occurring samples (Table 1). When the 3310 cm-1 absorption is strong, additional weak bands at 3233 and 3185 cm-1 are observed that are identical to the type II spectra of the synthetic corundums (light blue to blue sapphire, “amethyst“-colored sapphire) reported by Beran (1991). In the spectra of the samples with the greatest intensity, additional weak bands are observed at 3395 and 3367 cm-1.

A significant correlation exists between the color and the OH-band intensities. Blue to dark blue sapphires show the highest amount of OH; the OH content of light blue sapphires is significantly lower. This is especially evident in the zoned crystals from Laos showing varying colors of dark blue to bluish-gray. Smith (1995) also observed the greatest OH concentrations in blue sapphires from basaltic sources such as Australia. Table 1 shows that all corundums with the higher absorption coefficients have blue hues. The highest absorption coefficient value of 0.7 cm-1 was observed for a blue Australian sapphire and blue faceted sapphires (that may have been heat-treated). Also some greenish-blue and violet sapphires show relatively strong absorption bands. Only from one ruby sample was a very weak absorption at 3310 cm-1 observable.

Regarding the large number of samples available from the Montana mines (Brownlow and Komorowski, 1988; Mychaluk, 1995), most of the sapphires from the Dry Cottonwood Gulch show significant absorptions due to OH.  Sapphires from the gemstone mines in Australia (Guo et al., 1995) reveal the most intense absorption bands, samples from Sri Lanka show very limited amounts of OH, samples from Laos are characterized by a distinct OH zoning. Absorption coefficients of sapphires relatively rich in OH are concentrated at around 0.15(2) cm-1. 	Examination of a suite of Montana samples makes it evident that the absorption bands of heat treated dark blue sapphires are more intense than the bands of the corresponding untreated material.  This supports previous suggestions that hydrogen enters mineral structures in an oxidation-reduction reaction, expressed by Fe3+ + O2- + ½ H2 = Fe2+ + OH-, in which  Fe3+ is reduced by hydrogen producing an OH group in its immediate vicinity (Skogby and Rossman 1989; Redhammer et al. 1993).

Measurements with polarized radiation on natural crystals confirm that the orientation of the OH dipole is perpendicular to [0001] as previously determined on synthetic material (Eigenmann et al. 1972; Volynets et al., 1972; Beran, 1991; Moon and Phillips, 1991).  All OH bands show maximum absorptions when the electric vector of the polarized radiation vibrates perpendicular to the c-axis (Fig. 1). A plausible model of OH incorporation, based on polarized measurements, can be developed under the assumption of an incomplete occupancy of the cation positions. Assuming vacancies in the Al lattice, in a model developed by Beran (1991), the OH dipole oriented perpendicular to the c-axis is coordinated to two Al atoms forming groups of face-sharing Al2(OH)O8-double octahedra.  In this model the splitting of the triplet band with maxima at 3310, 3230 and 3185 cm-1 is mainly controlled by vacancies and not by coloring cations.  Moon and Phillips (1991) investigated the thermal behavior of the OH triplet band in a series of heating experiments on synthetic corundum and assigned the OH absorptions to different types of (TiAlVAlOHO) defect clusters.

Amount of OH

The absolute amount of OH can be determined from the total integrated areas of the OH bands by using the expression

Abstot = I  ×  t  ×  concentration                                     (1)

where Abstot is the total integrated intensity of the OH bands (as discussed in Bell et al. 2003);  t is the thickness in cm, concentration is in molesH2O/liter and I is the experimentally determined integral molar absorption coefficient. Note that the concentration of all hydrous species is reported as H2O.

The hydrogen concentration can only be accurately determined, if the matrix specific integral molar absorption coefficient, I in equation (1), is known. Comparing the OH absorbance intensity of the natural sapphires with those of synthetic samples reported by Beran (1991), it is evident that the OH content of most of the natural material is in the same order of magnitude as most of the synthetic samples.  The absolute amount of OH absorption is low, indicating that an absolute measurement of the OH in corundum will probably not be possible with current absolute calibration methods.  Instead, we must indirectly determine the OH content through calibration of the OH band intensity with other standards which we will assume will reasonably represent the behavior of OH in corundum.

Beran (1991) proposed a calibration of the OH content of sapphire using kyanite with small hydrogen contents as a standard mineral. Similar to corundum, the kyanite structure contains oxygen atoms arranged in a slightly distorted close-packed cubic array and its IR spectrum shows comparatively sharp OH absorptions at around 3380 and 3270 cm-1 centered in a similar energy region as observed in corundum. The hydrogen concentrations thus calculated for the synthetic sapphires varied from 10 to 30 wt.ppm (expressed as H2O).

Subsequently, the accuracy of the kyanite calibration of Beran (1991) was questioned by Bell et al. (2004 in review) who re-analyzed kyanite by nuclear reaction analysis (NRA) and obtained a different calibration constant which indicated that the earlier work overestimated the OH content in kyanite by a factor of about 18.  The integral molar absorption coefficient, I, derived in the Bell et al. (2004) kyanite calibration is I = 32900 L × mol-1 × cm-2. This is between the corresponding values for olivine (I = 28450) and clinopyroxene (I = 38300) (Bell et al. 2003; Bell et al. 1995).

The most OH-rich corundum in Table 1 that is not likely to have been heat-treated is GRR1020-A. From Fig. 1, the Abstot  (defined as Abs||c + 2 × Abs(c)  is 21.68. The amount of H2O bound in the corundum is determined from the concentration, 21.68 / 32900 = 0.000659 moles H2O per liter (4000 g) of corundum. That corresponds to 0.000659 × 18 = 0.0119 grams H2O per 4000 grams corundum, which corresponds to 3.0 ppm. The new kyanite calibration puts our highest observed hydrogen concentrations in natural corundum crystals at about 3 ppm (by weight as H2O) and for most crystals at 0.5 ppm or less. This value excludes inclusions of hydrous phases.

Approximations such as proposed by Paterson (1982) and modified by Libowitzky and Rossman (1997) provide an alternative way to estimate the integral molar absorption coefficients based on the energy of the absorption. For example, Paterson’s (1982) relationship was used by Kronenberg et al. (2000) for the evaluation of the OH defect concentration in their hydrothermally treated corundums. The revised calibration of Libowitzky and Rossman leads to an estimate of the H2O in corundum GRR1020-A of about 0.9 wt.ppm H2O using the Abstot derived in the previous paragraph. While this is only an estimate of the amount of OH in corundum, it does serve to confirm the low concentrations of OH found in this phase to date. It is interesting to note that the I values obtained on the basis of the NRA kyanite calibration are lower, by about a factor of 4, than the values following from the IR calibration trend given by Libowitzky and Rossman (1997) and that a similar factor was reported by Maldener et al. (2001) for rutile and cassiterite and for pyrope in Libowitzky and Rossman (1997). The origin of the large differences between the kyanite calibration of Beran and Götzinger (1987) and the one by Bell et al. (2004) may be explained by the nature of the samples analyzed. The 1987 analysis required 300 mg of extremely pure kyanite. In retrospect, it is highly probable that the high hydrogen content that resulted in the calculation of a low I value was due to the presence of undetected, submicroscopic inclusions of hydrous alteration products and strongly absorbed water located in incipient cleavages on fractured ends of grains.

As an alternative to using the total integrated intensities, it is possible to estimate the concentration of H2O from the intensity of the 3310 cm-1 OH absorption bands (A). It is related to the concentration of the OH groups (c) by the molar absorption coefficient (() and the thickness of the samples (t). This relation is expressed by Beer’s law

A = ((c × c × t                                        (2)

From the data in Fig. 1, ((c is determined to be 1077 from the E(c spectrum of Fig. 1. Because the spectrum of corundum is generally similar from sample to sample, and because the intensity is primarily in the E(c direction, the content can be estimated from a single spectrum using the kyanite calibration discussed above.  The same calibration could be used for an unpolarized spectrum taken on a (0001) slab of corundum.

A different calibration is obtained from unpolarized spectra taken on ac slabs of corundum. In this case, (unpol, obtained from the unpolarized spectrum of sample 1020-A, is 247. Use of (unpol should be considered less accurate because of partial polarization effects in most infrared spectrophotometers, even when used without polarizers. In the case of our instrument, rotating the sample 90 degrees about the axis of the light path resulted in a 30% reduction in the absorbance of the 3310 cm-1 band in the unpolarized spectrum. Also noteworthy is the fact that the intensity of an unpolarized spectrum from a sample of unknown orientation can vary by a factor of 4 depending on the true orientation of the sample.

Hydrous Mineral Inclusions

All of the calibrations above do not include hydrous inclusions, yet such inclusions are abundant in many samples of corundum. Guo et al. (1995), Smith (1995) and references therein describe mineral inclusions in gem-quality sapphires mainly from Australian and Asian occurrences. Inclusions of hydrous minerals frequently occur in corundum and contribute to its IR spectrum. We observe the spectroscopic features of many of the hydrous minerals reported by Smith (1995) in gem rubies. Features of kaolinite, chlorites, diaspore, boehmite and goethite are the ones we most commonly encountered.  We find no correlation between the intensity of the OH absorptions and the optical clarity of the crystals. Spectra taken through turbid portions of crystals show distinct groups of absorption bands centered at different wavenumbers within the OH fundamental region. Typical examples are shown in Fig. 2. The significant absorption peak of spectrum a) is due to the presence of fine-grained goethite dispersed along fracture surfaces in the crystal which causes the yellow color of a corundum sample from Sri Lanka. The absorptions of chlorite group minerals are frequently observed in sapphires from Montana and Tanzania (Fig. 2 b). The characteristic absorptions of diaspore with a maximum centered at around 2900 cm-1 indicate the source of turbidity in rubies from Tanzania (Fig. 2 d). The most common phases identified from the spectrum of turbid parts of corundum crystals are kaolinite group minerals which show how IR spectroscopy is a very useful method for the identification and characterization of very small amounts of extremely fine-grained contaminating mineral phases.

Acknowledgements

We wish to thank the following people for kindly providing corundum samples for this study: Joe Borden, E. Buzz Gray, Michael Gray, George Harlow, Tony Kampf, Robert E Kane, Peter Keller, H. F. Kennedy, Elbert King, Julius Petch, Robert Weiser and Ray Weldon. This investigation was supported by the Austrian Fonds zur Förderung der wissenschaftlichen Forschung P8122-GEO and the National Science Foundation (USA) grants EAR-9218980 and EAR-0125767.

References Cited

Bell DR, Ihinger PD, Rossman GR (1995) Quantitative analysis of hydroxyl in garnet and pyroxene. American Mineralogist 80: 465-474

Bell DR, Rossman GR, Maldener J, Endisch D, Rauch F (2003) Hydroxide in olivine: A quantitative determination of the absolute amount and calibration of the IR spectrum. Journal of Geochemical Research, 108(B2), 2105, doi:10.1029/2001JB000679, 2003

Bell DR, Rossman GR, Maldener J, Endisch E, Rauch F (2004) Hydroxide in kyanite: A quantitative determination of the absolute amount and calibration of the IR spectrum. (in preparation)

Belt FR (1967) Hydrothermal ruby: Infrared spectra and X-ray topography. J Appl Phys 38: 2688-2689

Beran A (1991) Trace hydrogen in Verneuil-grown corundum and its colour varieties - an IR pectroscopic study. Eur J Mineral 3: 971-975

Beran A, Götzinger MA (1987) The quantitative IR spectroscopic determination of structural OH groups in kyanites. Mineral Petrol 36: 41-49

Beran A, Zemann J (1971) Messung des Ultrarot-Pleochroismus von Mineralen. XI. Der Pleochroismus der OH-Streckfrequenz in Rutil, Anatas, Brookit und Cassiterit. Tschermaks Mineral Petrogr Mitt 15: 71-80

Brownlow AH, Komorowski J-C (1988) Geology and origin of the Yogo sapphire deposit, Montana. Econ Geol 83: 875-880

Eigenmann K, Kurtz K, Günthard HH (1972) Solid state reactions and defects in doped Verneuil

sapphire. Helvet Physica Acta 45: 452-480

Emmett JL, Scarrratt K, McClure SF, Moses T, Douthit TR, Hughes R, Novak S, Shigley JE, Wang W, Bordelon O, Kan RE (2003) Beryllium diffusion of ruby and sapphire. Gems & Gemology 39: 84-135

Guo J, O’Reilly SY, Griffin WL (1995) Corundum from basaltic terrains: a mineral inclusion approach to the enigma. Contr Mineral Petrol 122: 368-386

Hammer VMF, Beran A (1991) Variations in the OH concentrations of rutiles from different

geological environments. Mineral Petrol 45: 1-9

Kronenberg AK (1994) Hydrogen speciation and chemical weakening of quartz. In: Heaney PJ et al (eds) Silica. Rev Mineral 29, Miner Soc Amer, pp 123-176

Kronenberg AK, Castaing J, Mitchell TE, Kirby SH (2000) Hydrogen defects in (-Al2O3 and water weakening of sapphire and alumina ceramics between 600 and 1000°C - I. Infrared characterization of defects. Acta mater 48: 1481-1494

Libowitzky E, Rossman GR (1997) An IR absorption calibration for water in minerals. Am Mineral 82: 1111-1115

Maldener J, Rauch F, Gavranic M, Beran A (2001) OH absorption coefficients of rutile and cassiterite deduced from nuclear reaction analysis and FTIR spectroscopy. Mineral Petrol 71: 21-29

Moon AR, Phillips MR (1991) Defect clustering in H,Ti:-Al2O3. J Phys Chem Solids 52: 1087-1099

Moon AR, Phillips MR (1994) Defect clustering and color in Fe,Ti:-Al2O3. J Am Ceram Soc 77: 356-367

Mychaluk KA (1995) The Yogo sapphire deposit. Gems Gemology 31: 28-41

Paterson MS (1982) The determination of hydroxyl by infrared absorption in quartz, silicate glasses and similar materials. Bull Mineral 105: 20-29

Peretti A, Schmetzer K, Bernhardt H-J, Mouawad F (1995) Rubies from Mong Hsu. Gems  Gemology 31: 2-26

Potter RM, Rossman GR (1979) The tetravalent manganese oxides: identification, hydration, and structural relationships by infrared spectroscopy. Am Mineral 64: 1199-1218

Redhammer GJ, Beran A, Dachs E, Amthauer G (1993) A Mössbauer and X-ray diffraction study of annites synthesized at different oxygen fugacities and crystal chemical implications. Phys Chem Minerals 20: 382-394

Skogby H, Rossman GR (1989) OH in pyroxenes: An experimental study of incorporation mechanisms and stability. American Mineralogist 74: 1059-1069

Smith CP (1995) A contribution to understanding the infrared spectra of rubies from Mong Hsu, Myanmar. J Gemmology 24: 321-335

Smith CP, Kammerling RC, Keller AS, Peretti A, Scarratt KV, Khoa ND, Repetto S (1995) Sapphires from southern Vietnam. Gems Gemology 31: 168-186

Vlassopoulos D, Rossman GR, Haggerty SE (1993) Coupled substitution of H and minor elements in rutile and the implications of high OH contents in Nb- and Cr-rich rutile from the upper mantle. Am Mineral 78: 1181-1191

Volynets FK, Sidorova YA, Stsepuro NA (1972) OH-groups in corundum crystals grown by the Verneuil technique (in Russian). J Appl Spectr 17: 1088-1091

Authors’ addresses: A. Beran, Institut für Mineralogie und Kristallographie, Universität Wien-Geozentrum, Althanstrasse 14, A-1090 Wien, Austria; G.R. Rossman, Division of Geololgical and Planetary Sciences, California Institute of Technology, Pasadena, CA 91125-2500, USA

Table 1. Localities, color, wavenumber positions and OH absorption coefficients for corundum. The absorption coefficient ( is defined by the absorbance A = log[I0/I] divided by the thickness of the crystal t measured in cm (( = A/t)

--------------------------------------------------------------------------------------------------------------------------------------

Sample	Locality	Number of Samples	Absorption coefficient

and Color	per cm at 3310 cm-1

(unpolarized)

LA 1386	Yogo Gulch,	2  yellowish-grey	0.0

Judith Basin Co.,	1  greenish-grey	0.0

Montana	1  greyish-yellow	0.006

1  greenish-yellow	0.0

2  yellow	0.0

1  yellow/greenish-blue	0.0

LA 18947	Yogo Gulch,	1  light greenish-blue	0.0

Judith Basin Co.,	1  blue/greenish-grey	0.006

Montana

LA 16700	Yogo Sapphire Mine,	2  light blue	0.0 - 0.008

Judith Basin Co.,	3  blue	0.0

Montana

LA 16699	Dry Cottonwood Gulch,	1  colorless/yellow	0.006

Silver Bow Co.,	2  light greyish-blue	0 - 0.003

Montana	4  greyish-blue	0.01 - 0.012

LA 18946	El Dorado Bar,	2  greyish-blue	0.01 - 0.016

Lewis & Clark Co.,	3  bluish-grey	0.0

Montana	1  greenish-blue	0.01

2  light blue	0.01

2  yellow	0.0

1  rose	0.0

GRR 849	Rock Creek,	2  colorless	0.0

Montana	2  light blue	0.0

1  greenish-blue	0.007

2  light yellow	0.0

2  rose	0.0

GRR 675	Near Coal Creek,	1  colorless	0.0

Montana	1  yellow	0.0

GRR 836	Montana	5  light blue	0.0

1  light greyish-blue	0.0

3  light greenish-blue	0 - 0.05

LA 12229	Macon Co.,	1  dark blue	0.12

North Carolina	1  dark blue	0.16

LA 12230	Macon Co.,	2  greenish-grey	0.0

North Carolina	1  bluish-grey	0.085

1  greenish-blue	0.0

GRR 1334	Malacheta, Brazil	1  blue (faceted)	0.33

GRR 1335	Goiaz, Brazil	1  light blue (faceted)	0.24

GRR 1054	Queensland, Australia	4  greenish-blue	0.03-0.17

GRR 1020	Australia(?)	1  blue	0.15

2  dark blue	0.1 - 0.16*

GRR 1047	Australia	1  blue	0.17

LA 6908 	Australia	1  bluish-grey/yellow	0.0

1  greenish-blue/yellow	0.01

1  blue	0.49

GRR 906	Kenya	1  violet	0.06

1  rose	0.0

2  red	0.0

GRR 788	Nigeria	1  dark blue/light blue	0.14

(zoned)

GRR 890	Umba Valley, Tanzania	2  violet	0 - 0.015

1  light blue	0.015

1  blue	0.028

1  bluish-green	0.0

1  yellow	0.0

1  red	0.0

GRR 730	Tanzania	1  violet	0.015

1  blue	0.025

1  yellow	0.0

1  rose	0.01

2  red	0 – 0.025

GRR 838	Tanzania	1  colorless	0.0

2  light violet	0.015

1  violet	0.015

2  violet/grey	0.02 - 0.03

1  light violet/yellow	0.015

2  yellow/light blue	0.02 - 0.027

1  yellow	0.03

GRR 1045	Ratnapura, Sri Lanka	1  colorless	0.0

GRR 540	Sri Lanka	1  rose	0.003

GRR 673	Sri Lanka	3  yellow	0.0

GRR 674	Sri Lanka	1  colorless/yellow	0.0

1  bluish-grey/yellow	0.0

1  light grey/red	0.0

LA 19734	Sri Lanka	3  colorless	0.0

1  colorless/yellow	0.0

1  light blue	0.006

LA 19750	Sri Lanka	3  colorless	0.0

2  greyish-blue	0 - 0.01

2  yellow	0.0

LA 6906 	Sri Lanka	3  colorless/yellow	0.0

1  light yellow	0.0

1  grey	0.0

GRR 736	Chantaburi, Thailand	1  bluish-grey	0.0

1  blue	0.048

1  red	0.0

GRR 1870	Ban Houayxay, Laos	4  greenish-blue	0 - 0.025

1  bluish-grey	0.01

3  blue	0.01 - 0.023

1  dark blue	0.15

1  green	0.0

1  brownish-green	0.0

1  brownish-yellow	0.01

(zoned crystals)

GRR 662	SE Asia	1  colorless	0.0

2  greyish-blue	0.01 – 0.10

GRR 1382	SE Asia	1  colorless	0.0

GRR 1021	Cambodia	1  brown/yellow	0.0

GRR 1065	Greenland	2  red	0.0

---------------------------------------------------------------------------------------------------------------------

* GRR 1020; Absorption coefficient per cm at 3310 cm-1 (polarized E (c) = 0.42 - 0.71

----------------------------------------------------------------------------------------------------------------------

Figure Captions

Fig. 1. Polarized single-crystal spectra in the OH stretching vibrational range of a 4.29 mm thick blue sapphire GRR 1020 presumed to be from Australia, with the electric vector of the polarized radiation vibrating perpendicular and parallel to the c-axis. This spectrum is representative of the sharp OH bands in all natural corundums, but of greater intensity than most.

Fig. 2. Unpolarized spectra in the OH stretching vibrational range of corundum, taken through turbid crystal parts. (a) OH absorption features of goethite – GRR 673, (b) chlorite group minerals, GRR 838 from Umba River Valley, Tanzania), (c) kaolinite group minerals – LA 16699, and (d) diaspore – GRR 730.