Table 1.  Sample details and the results of NRA and IR H2O analyses.

_______________________________________________________________________________________________________

Sample number	H105650*		H85943*	LTL-3  	 	FSM-15

Locality	Itabira, Minas Gerais                                             Letlhakane Mine      Frank Smith Mine

Brazil	Brazil	Botswana		South Africa

H2O (ppm by weight by NRA)	4 	22 	27		230

IR integ/cm  ()	46	165	803 		1560

IR integ/cm (	1	142	393		780

Peak height per mm at 3380 cm-1	0	0.371	0.567		1.679

Sum of 5 peak heights in beta	0	0.67	1.66		3.73

______________________________________________________________________________________

* Harvard University Mineral Museum Sample Number